1. Prep pouring log with date
2. Mark slides, cuvettes, and dogbone slots with ratios
3. Open jars
4. Clean metal spatulas with DI water
5. Measure out the appropriate amount of Part B into a cup with a pipette
6. Measure out the appropriate amount of So-Flex II into the same cup as the Part B with a pipette
7. Mix So-Flex II and Part B with a metal spatula
8. Vacuum So-Flex/Part B cup
9. Vacuum Part A Jar
10. Dispense Part A into the Part B cup with a wooden spatula
11. Mix with a metal spatula
12. Vacuum
13. Pour into dogbone and scrape if needed
14. Pour into cuvettes
15. Pour onto slides
16. Vacuum seal jars again